## Slide 1: Sample composition
AlN/GaN-on-SiC
SiC substrate
AlGaN (110 nm)
AlGaN (990 nm)
Ti rich layer (100 nm)
Polycrystalline Pt-Au (360 nm)
Amorph. deposited Pt (1-2 µm)
SiN cap (6 nm) / AlN barrier (5 nm)
GaN channel (150 nm)
200 nm
Left: A top-view image of a lamellae produced using focus ion beam technique. The sample was glued to a gold coated sample holder. Right: a zoomed image of the region of interest, where layers of different materials locate (framed region in left panel). As shown, the region consist of layers with different electrical properties: metallic (Pt, Au, Ti, with total thickness of about 2 micron), semiconducting AlGaN+GaN (total thickness of about 1.3 micron) and dielectric SiC substrate.
A 39 x 15 µm2
lamella
Au-coated sample holder

## Slide 2: Thin semiconducting lamella All images and graphs are from the dataset: XYScanNano_60.0x70.0um_120x140px_Al_GaN on SiC1_217.41_200409_010259.gwy
SiC+GaN
GaN?
Top panels: A 2D topography map and a profile extracted from this map along the dashed white line. Bottom panels: A 2D map of the magnitude of S11 and a similarly extracted profile. The thin lamella is visible in both topography and electrical maps. However, it is difficult to determine the position of GaN/AlGaN multilayers from SiC from profies extracted from these maps (right panels). The position of the film edges cannot be determined precisely because of the tip convolution. In turn, it is possible to guess the position of the GaN/AlGaN layers. Moreover, the lack of contrast in the electrical measurement between GaN/AlGaN and SiC is attributed to the small difference in electrical properties of these materials (both is non-conducting and have similar dielectric constants: εGaN=5.3 εSiC=6.52 at high frequency [1]).
[1]: Bougrov V, et al., Properties of Advanced semiconductor materials GaN, John Wilye & Sons, Inc. New York, 2001

## Slide 3: Thin semiconducting lamella: sample damage
Before
After
a)
b)
a) and b) Scanning electron microscopic (SEM) image taken before and after SMM measurements. Black dashed frames in a) and b) points at the zone of interest, where multilayers stay. However, as shown in b), this region was damaged during the SMM measurements. We expect that the tip, which is in contact with the sample, removed part of the metallic layers deposited during the production of this lamella. c) and d) are SEM images zoomed in the region of interest. The scale bars in a), b), c) and d) are 5 µm, 5 µm, 500 nm and 1 µm respectively.
AlGaN
SiC
AlGaN
Au
Pt
c)
SiC
d)

## Slide 4: Measurement conditions

## Slide 5: Measurement conditions

## Slide 6: Measurement conditions

## Slide 7: Measurement conditions

## Slide 8: Measurement conditions

## Slide 9: Measurement conditions

## Slide 10: Measurement conditions